# Developments of High-Resolution/High voltage/3D environmental TEMs    and their Applications in Materials Science

Nobuo Tanaka1,2

1Ecotopia Science Institute, Nagoya University, Nagoya, Japan

2Nanostructures Laboratory, Japan Fine Ceramics Center, Nagoya, Japan

The invention of differential pumping systems[1-4] and membrane type environmental cells has enabled us to achieve high-resolution transmission electron microscope (HRTEM) images of specimens in a gaseous environment. Many successful in-situ HRTEM observations have been reported using such environmental transmission electron microscopes (ETEM) since 1997[1]. ETEM will be of much interest for research into nm-sized catalysts, ceramics and biomedical materials, particularly in next few years.

For maturing of the ETEM technique, we have recently developed/installed two types of advanced ETEM in Nagoya University and Japan Fine Ceramics Center. One has a retractable differential pumping E-cell, which was designed for minimizing the missing wedge to improve the accuracy of electron tomography. The acceleration voltage for 3D ETEM is in the range of 800-1000 kV for thick specimens of real devices (300nm to 10μm) [4]. Another major demand for ETEM is in catalysis. Spatial and time-resolution of the HRTEM were explored for dynamic observation of single atom behavior, which is necessary for understanding chemical reactions. The ultra high-resolution ETEM using an environmentally modified TITAN gives a real-time video recording with information transfer out to 0.1nm, time-resolution below 0.2 seconds and accelerating voltage range from 80kV to 300kV.  In the present study, we report examples of in-situ gas study and three-dimensional analysis using a newly developed 1MV 3D ETEM (JEM-1000KRS, Nagoya Univ./JEOL) and an ultra high-resolution ETEM (JFCC/ FEI).

We show a 3D tomogram of a carbon micro-coil prepared by the CVD method from acetylene gas and nickel powders on graphite substrates[5]. More than 100 images were recorded at 1MV using a 360 degree single-axis rotation holder. The image reconstruction was performed by software using the SIRT method (JEOL). Sections from the 3D reconstruction clearly show the cross-sections of the fiber, which provide information about the CVD growth of the coil. The data of single platinum atoms visualized using the aberration-corrected ETEM are also presented. Pt/a-carbon is a typical electrode catalyst for a proton exchange membrane fuel cell (PEMFC)[6]. These results indicate that in-situ aberration corrected TEM observation is useful for visualizing and identifying the sintering mechanisms.

Professors K. Sasaki, K. Saitoh and J. Yamasaki, Drs. S. Arai, K. Yoshida, A. Bright, Y. Sasaki, and Mr. X. Zhang are acknowledged for contribution on this project.

References

[1] E. D. Boyes et al., Ultramicrosc. 67 (1997) 219.

[2] P. L. Gai et al., Top. Catal. 21 (2002) 161.

[3] H. Hanzen et al., Jour. Catal. 216 (2003) 155.

[4] N. Tanaka et al. (2009), Proc. Int. Cong. Microsc. (Rio de Jaineiro), I9-2.

[5]S. Motojima et al., Appl. Phys. Lett., 54(1989) 1001.

[6] K. Yoshida et al., J. Electron Microsc., 61(2012), in print.